## Slide 1: Magnetron sputtered titania and carbon fiber cloth composite and its application in electrochemical supercapacitors
APPLICATIONS OF CHEMISTRY
IN NANOSCIENCES
AND BIOMATERIALS ENGINEERING
NanoBioMat 2022 – Summer Edition
22-24 June 2022
Kozlov Aleksei P.1,2*, Arkhipova Ekaterina A.1, Savilov Serguei V.1
1Chemistry Department of M. V. Lomonosov Moscow State University
2Moscow Aviation Institute (National Research University)
kozlov.aleksei.p@gmail.com

## Slide 2: Introduction
2
APPLICATIONS OF CHEMISTRY IN NANOSCIENCES AND BIOMATERIALS ENGINEERING
NanoBioMat 2022 – Summer Edition 22-24 June 2022
noaa.gov; teriin.org
futurebridge.com; mdpi.com; 10.1002/advs.201500319

## Slide 3: Creating composite material for supercapacitor application
3
APPLICATIONS OF CHEMISTRY IN NANOSCIENCES AND BIOMATERIALS ENGINEERING
NanoBioMat 2022 – Summer Edition 22-24 June 2022
Commercial Carbon Fiber cloth
Titania was coated on Carbon Fiber using RF magnetron sputtering
Characterization:
Scanning Electron Microscopy, Raman Spectroscopy, X-Ray Diffraction, X-Ray Photoelectron Spectroscopy, Electron Paramagnetic Resonance, Thermal analysis, Pore Analysis, Electrochemical analyses

## Slide 4: Scanning Electron Microscopy
Ti coated Carbon Fiber
Carbon Fiber
4
APPLICATIONS OF CHEMISTRY IN NANOSCIENCES AND BIOMATERIALS ENGINEERING
NanoBioMat 2022 – Summer Edition 22-24 June 2022

## Slide 5: Raman Spectroscopy, X-Ray Diffraction
X-ray diffraction demonstrates broad peak at 2θ≈36°, suggesting a (101) plane of Rutile, polymorph of TiO2;
Raman spectrum of carbon region shows distinct D and G bands, typically accociated with defects and in-plane vibrations of sp2-carbon, respectively.
5
APPLICATIONS OF CHEMISTRY IN NANOSCIENCES AND BIOMATERIALS ENGINEERING
NanoBioMat 2022 – Summer Edition 22-24 June 2022

## Slide 6: X-Ray Photoelectron Spectroscopy, Electron Paramagnetic Resonance
Survey spectrum shows 3 major elements, C, O, Ti and negligible amount of N;
C1s region suggests that Carbon Fiber is functionalized by oxygen-containing groups;
Ti2p region demonstrates high amount of Ti4+ and almost no Ti0
EPR showed no signal of Ti3+
6
APPLICATIONS OF CHEMISTRY IN NANOSCIENCES AND BIOMATERIALS ENGINEERING
NanoBioMat 2022 – Summer Edition 22-24 June 2022

## Slide 7: Thermal analysis
20-450 °C region: prolonged water evaporation from material, resulting in 2.5% mass loss;
450-700 °C region: being also highly exothermic, shows a rapid mass loss, from 97.5 to 12%, suggesting a reaction of carbon oxidation by air oxygen and the TiO2 loading content of 12%.
700-900 °C region with mass increase of 1% can be attributed to oxidation of residual metallic Ti.
7
APPLICATIONS OF CHEMISTRY IN NANOSCIENCES AND BIOMATERIALS ENGINEERING
NanoBioMat 2022 – Summer Edition 22-24 June 2022

## Slide 8: Pore analysis
According to the IUPAC pore classification these are the type I isotherms, therefore material is microporous (pore size <5 nm). Isotherms demonstrate a hysteresis loop of type H4, suggesting a “slit” pore type.
Applied pore calculation method QSDFT estimates specific surface area value of 1210.7 m2 g-1, 12,5% less than that of initial Carbon Fiber.
Pore size distribution shows that majority of pores are micropores.
8
APPLICATIONS OF CHEMISTRY IN NANOSCIENCES AND BIOMATERIALS ENGINEERING
NanoBioMat 2022 – Summer Edition 22-24 June 2022

## Slide 9: Supercapacitor performance
9
APPLICATIONS OF CHEMISTRY IN NANOSCIENCES AND BIOMATERIALS ENGINEERING
NanoBioMat 2022 – Summer Edition 22-24 June 2022
Electrochemical Impedance Spectroscopy
Cyclic Voltammetry
Specific Capacitance – Scan Rate
Cycle Efficiency

## Slide 10: Conclusion
Titania was successfully applied on the Carbon Fiber cloth by magnetron sputtering, exhibiting an uniform coating;
Titania was found to be in Rutile polymorph, with negligible amounts of metallic Ti. Ti3+ centers were not detected;
Carbon Fiber demonstrated both rich O-containing surface functionalities and microporous structure with a developed surface area, that were mostly inaffected by titania coating;
Resulting Titania coated Carbon Fiber composite material showed better impedance response, electrochemical activity, cycle efficiency compared to initial Carbon Fiber, and comparable specific capacitance.
Thank you for your attention!
10
APPLICATIONS OF CHEMISTRY IN NANOSCIENCES AND BIOMATERIALS ENGINEERING
NanoBioMat 2022 – Summer Edition 22-24 June 2022
Acknowledges: Korobeinikov Evgeniy, Chekmaryov Dmitriy, Oksana Isaikina, Maslakov Konstantin, Kupreenko Stepan, Suslova Evgeniya.